The procedure to be followed shall be as described in AS 2891.7.1, Determination of maximum density of asphalt - Water displacement method, except where modified or clarified as shown below.

In Clause 6(a)

Replace 2 with 4

In Clause 7, replace Table 1 with the following:

Replace ‘two test portions’ with ‘one test portion’

| Table 1 |  |
| --- | --- |
| MINIMUM MASS OF TEST SAMPLE |  |
| Nominal size of mix mm | Minimum mass of test sample g |
| < 10 | 1 000 |
| 10 | 1 500 |
| 14 | 1 500 |
| >20 | 2 000 |

Clause 10

Replace ‘two test portions’ with ‘test sample’.

PRECISION

The uncertainty of measurement has been determined as ± 0.008 tonnes/m3 of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025.

Uncertainty of Measurement determined by and for DPTI Technical Services Group, Field Services Section.

DOCUMENTATION

Complete form AS 2981.7.1-1