- 1.0	SCOPE

- This method shall be used to calculate the parts cutter per 100 parts bitumen (v/v) in bituminous binder in the range 0-8 parts cutter.

- 2.0	REFERENCES

- Preparation of a Bituminous Binder Cutting Chart, TP668.

- Determination of Viscosity by Haake Viscobalance, TP652.

- Residual Bitumen for Pavements, AS 2008.

- 3.0	DEFINITIONS

- Nil.

- 4.0	APPARATUS AND MATERIALS

- 4.1	Apparatus

- Apparatus per Procedure TP652, 4.1.

- 4.2	Materials

- Class 170 bitumen as used to prepare the bituminous binder in the field

- 5.0	SAMPLING AND SAMPLE PREPARATION

- 5.1	Sampling

- The Class 170 bitumen and the bituminous binder shall be sampled in accordance with AS 2008, Appendix B.

- 5.2	Sample Preparation

- The Class 170 bitumen and the bituminous binder shall be prepared in accordance with Procedure TP652.

- 6.0	PROCEDURE TO BE FOLLOWED

- 6.1	The viscosities of the Class 170 bitumen and the bituminous binder shall be determined at 60°C in accordance with Procedure TP652.

- 6.2	Using the appropriate cutting chart (Procedure TP668), determine the parts cutter in the bituminous binder.

- Note 	Where a sample of Class 170 bitumen is unavailable, a value of 170 Pa.s shall be used as the reference point.

7.0	CALCULATIONS

Nil.

8.0	PRECISION

No precision data available at this time.

- 9.0	REPORTS AND DOCUMENTATION

9.1	Reports

Report the parts cutter in the bituminous binder to the nearest 0.1 part.

9.2	Documentation

Form TP667-1.

Department of Planning, Transport & Infrastructure

19 Bridge Road Walkley Heights Ph (08) 8260 0230, GPO Box 1533, Adelaide SA  5001

Technical Services Group

Procedures - Laboratories

Method for Calculation of the Parts Cutter

in Bituminous Binder

Material: .....................................................  	Sample Id:  ..................…..........................................

Viscosity of Bulker/Storage/ex PRA Sample* (Pa.s)		_ _ _ _ _ _ _ _ _ _

Sample Id/Certificate No.*		_ _ _ _ _ _ _ _ _ _

Viscosity of Bituminous Binder at 60°C (Pa.s)		_ _ _ _ _ _ _ _ _ _

Date of TP668 Cutter Chart used		_ _ _ _ _ _ _ _ _ _

Parts Cutter/Flux* in Bituminous Binder		_ _ _ _ _ _ _ _ _ _

* Indicate as appropriate

Determined by _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _  Checked by _ _ _ _ _ _ _ _ _  Date _ _ _ _ _ _ _ _

Form TP667-1, Revn. 3.8