- 1.0	PURPOSE

- To provide procedures for the audit of the personnel, plant and procedures involved in the application of non-skid road marking paint for DPTI.

- 2.0	SCOPE

- These instructions pertain to the application of non-skid road marking paint by hand spray.

- 3.0	REFERENCES

AS/NZS 1580.301.1, Non-volatile content

AS/NZS 1580.107.1, Determination of wet film thickness from dry film mass.

AS/NZS 1742.3, Manual of Uniform Traffic Control Devices.

Road Traffic Act,

DPTI Specification: Part 245.3: Supply of Pavement Marking Materials - Crushed White Quartz for Non-Skid Paint.

TP344  Determination of Skid Resistance with the Griptester.

TP345  Determination of Skid Resistance with the British Portable Pendulum tester.

TP943  Determination of Quartz/ Paint Ratio, Non-skid Paint.

TP946  Quartz – Physical Properties

PC106  Traffic Management at Work Sites on Roads

4.0	DEFINITIONS

Non-skid road marking paint - a mixture of graded quartz and paint which, when applied to a pavement, provides a skid resistance in excess of 45BPN, when measured in accordance with TP344 or TP345.

- 5.0	PROCEDURE TO BE FOLLOWED

- 5.1	General

The aim of this procedure is to assess the effectiveness and consistency of application of non-skid paint. As this is subject to variation as a result of personnel, plant, and materials, each must be evaluated separately and as a whole with regard to the achievement of a satisfactory result on the road. All testing will take place at a test site designated by the Project Manager, Pavement Marking.

Note: site testing is conducted by Field Services, Pavement Marking Unit, while laboratory testing is conducted by Technical Services Group.

- 5.2	   PART 1 - Vehicle Compliance/ Traffic Control

    - Inspect the vehicle for compliance with the Road Traffic Act, and any other relevant regulations, and record the results in Part 1 of the documentation.

Note: This is an inspection only. Staff have no authority concerning non-compliance

Inspect the work-site to ensure compliance with the requirements of AS/NZS 1742.3, and assess the effectiveness of any traffic control in place. Refer to the relevant parts of PC106 Traffic Management at Work Sites on Roads.

- 5.3	PART 2 - Application

5.3.1	Record all company, operator, plant and equipment details.

    - Record the paint type being used and check for compliance against the DPTI list of approved products. Take a 500ml sample of paint, both with and without quartz, and an unopened bag of quartz.

5.3.3	Allow the operator to continue application, and record all observations. Make an assessment of the application in terms of over-spray, volume and consistency, and record. Assess the texture of markings applied against the reference standard plate, and record.

5.3.4	Request that operator spray 2 test panels of minimum dimensions 200 x 200mm, ensuring that the panels are representative of the work.

5.3.5  	All records from parts 1 & 2 to be kept by Field Services Pavement Marking Unit.

- 5.4	PART 3 - Laboratory Testing

5.4.1	Determine the quartz/ paint mixing ratio and density in accordance with TP943.

5.4.2	Determine the non-volatile content of the non-skid paint, in accordance with AS1580.301.1.

5.4.3	Allow the 2 test panels to dry overnight and then determine the mean wet film thickness in accordance with AS/NZS 1580.107.1.

5.4.4	Calculate the volume solids of the non-skid paint as follows:

- Volume Solids, VS = VP + (QR x 40)   x   100

100 +(QR x 40)

- Where: VP = volume solids of paint only

QR = mixing ratio, quartz/ paint (eg. 0.5)

5.4.5 	Calculate the dry film thickness of the non-skid paint as follows:

- Dry film thickness, Td = Tw x VS

100

- Where: Tw = wet film thickness from 5.3.8 above

VS = Volume Solids of non-skid paint

5.4.6	Check quartz for compliance with TP946.

5.4.7	Allow 7 to 28 days to elapse prior to determination of skid resistance, in accordance with the relevant DPTI procedures.

- 6.0	DOCUMENTATION

  - Field Services, Pavement Marking Unit:-

    - Complete  forms TP947 1-3

    - Complete form Non-Skid and Longitudinal Audit Checklist and Supply to Technical Services Group, Field Services TP947.4

  - Technical Services Group:-

- Complete Non-Skid Road-marking Report - Form TP947-4

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Audit - Non-Skid Paint

- Summary

- Audit No.:..........………………...........

Date of audit:     /     /

Location:………………………………………………………………………………………

…………………………………………………………………………………………………

- Operator Details

Company Name:............................................................................................……………

Contact Name:............................................................................................……………..

Contact No.   Telephone:........................…………….  Fax:........................................….

Operators: ......................................................................................................……………

- Plant Identification

Unit Make and Model : ..............................................    Registration No: ……………..

- ASSESSMENT

| ITEM | COMMENT* |
| --- | --- |
| Work-site management | Satisfactory/ unsatisfactory |
| Materials storage | Satisfactory/ unsatisfactory |
| Mixing | Satisfactory/ unsatisfactory |
| Application | Satisfactory/ unsatisfactory |
| Materials compliance | Satisfactory/ unsatisfactory |
| Skid resistance | Satisfactory/ unsatisfactory |

- cross out whichever is not applicable

This operation did/ did not comply with the requirements of DPTI.

Comments:   ……………………………………………………………………………………

- Testing Officer..........................................................................…………………………….

Form TP947-1, Revn. 3.7

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

- Audit - Non-Skid Paint

- PART 1 – WORK-SITE MANAGEMENT

| - ITEM | - OBSERVATION |
| --- | --- |
| - Rotating flashing lights |  |
| - Flashing arrowboard |  |
| - Vehicle signage |  |
| - Workers ahead |  |
| - Lane status |  |
| - Lateral shift |  |
| - Speed |  |
| - Cones |  |
| - Side road signage |  |
| - Safety jackets |  |
| - Ultra-violet management |  |

- Comments:................................................................................................……………

Testing Officer :.........................................…………………………………………….…

Form TP947-2, Revn. 3.7

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

- Audit - Non-Skid Paint

- PART 2 - APPLICATION

| ITEM | CHARACTERISTIC | OBSERVATION |
| --- | --- | --- |
| Mixing | Mixed in pot |  |
|  | Quartz measured |  |
|  | Paint measured |  |
|  | Mixing method |  |
|  | Quartz kept in suspension |  |
|  | Evidence of lumps |  |
| Flow Rate | Flow rate sufficient |  |
|  | Visible restrictions |  |
| Spraygun | Dripping |  |
|  | Fan width, mm |  |
|  | Overspray, mm |  |
|  | Application even |  |
| Operator | Application even |  |
| Texture | Against standards |  |

- Testing Officer:..................................………………………………………………..........……….

Form TP947-3, Revn. 3.7

| ## Location (Job ID / Schedule / Lot No / Road Name |  |  |  |  |  |  |  |  | ## Auditor |  | ## Audit No |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## Field Unit No. |  |  |  |  |  |  |  |  |  |  | ## Company |  |
| ## Operator |  |  |  |  |  |  |  |  |  |  | ## Date |  |
| ## Assessment Conducted: |  |  |  |  |  |  |  |  |  |  |  |  |
| - MATERIAL COMPLIANCE |  |  |  |  |  |  |  |  |  |  |  |  |
| - PROCESS AUDIT |  |  |  |  |  |  | TECHNICAL SERVICES GROUP REPORT NO: |  |  |  |  |  |
| PRODUCT AUDIT |  |  |  |  |  |  |  |  |  |  |  |  |
| ## Follow up: |  |  |  |  |  |  |  |  |  |  |  |  |
| - Audit Registered (date) |  |  |  |  |  |  |  |  |  |  |  |  |
| - Samples taken (date) |  |  |  |  |  |  |  |  |  |  |  |  |
| - Batch Number |  |  |  |  |  |  |  |  |  |  |  |  |
| - Panel Number |  |  |  |  |  |  |  |  |  |  |  |  |
| - Tin Samples |  |  |  |  |  |  |  |  |  |  |  |  |