Determination of the Moisture/Density Relationship of a Lime Stabilised Soil

The procedure shall be as described in Procedures AS 1289.5.1.1 or AS 1289.5.2.1 except where modified or clarified as shown below.

•	Hydrated lime shall be added to the soil/water mixture as required.

•	Moisture content shall be determined as a percentage of dry mass of soil plus lime.

•	Lime content is reported as a percentage of dry mass of soil.

•	The compaction test may be performed after a delay, depending on construction procedure simulation.