# 1.0	PURPOSE

This procedure describes the methods to be used to audit line marking processes, and to assess the procedures and plant used by contractors to provide the required levels of retroreflectivity, delineation and durability.

# 2.0	SCOPE

# These instructions pertain to the application of line marking by machine.

# 3.0	REFERENCES

AS/NZS 1580.202.1, Paints and related materials - Methods of test - Density

AS 1580.107.1, Determination of Wet Film Thickness from Dry Film Mass.

AS 1580.301.1, Non-volatile Content

AS 1742 Manual of uniform traffic control devices

TP907, Determination of Retro Reflectivity of Pavement Markings

TP908, Paint and Glass Bead Application Rates from Test Panels

TP946, Paint and Glass Bead Application Rates from Plastic Bags

4.0	DEFINITIONS

For the purposes of this procedure, line marking refers to the use of paint and glass beads only.

# 5.0	PROCEDURE TO BE FOLLOWED

# 5.1	General

The aim of this procedure is to assess the effectiveness and consistency of application of line marking. As this is subject to variation as a result of personnel, plant, and materials, each must be evaluated separately and as a whole with regard to the achievement of a satisfactory result on the road. A contract specific schedule shall be prepared for the number of Contractors and units operating during a contract.

All testing will take place at a test site designated by the Project Manager, Pavement Marking Unit. Auditing may include viewing contractor records.

  - Auditing

    - Audits shall be carried out as per Table 1, by Technical Services Group, Field Services Section

Table 1 - Audits

| Criteria | Data Source | Action |
| --- | --- | --- |
| Materials, paint and beads | Container Labels | Record, sample and test |
| Paint/ glass bead application rates | Paint wet film thickness records | View/ download/ document |
|  | Contractor material consumption records | View/ document |
| Placement, new markings | Relative to spotting | Measure/ Document |
| Placement, maintenance markings | Relative to existing markings | Measure/ Document |
| Dimensions | Stripe/ Module length | Measure/ Document |
| Retroreflectivity | Visual | View/ document |
|  | Measured | Measure |
| OHS&W and Work-site management | Observe | Document non-conformances |

5.2.2	Record all company and equipment details.

    - Record the details of the paint and glass beads being used, and check for compliance against the DPTI list of approved products.

    - Carry out sampling to verify material quality, at the sampling rate shown in Table 2. Where samples are taken by a Surveillance Officer, these shall be forwarded to the Technical Services Group, for testing.

Table 2 – Sampling Schedule

|  |  | Sampling |  |
| --- | --- | --- | --- |
| Product | Quantity | Labelling | Frequency |
| Paint | 2 x 500 ml | Contractor, Unit ID, Product, Batch No., Date | As per audit plan |

    - Test paint samples for compliance with specified requirements, in accordance with AS/NZS1580.202.1 and AS1580.301.1

    - Assess the effectiveness of the plant in applying one line over another, and delivering the line pattern within the specified tolerances.

    - Visually assess the effectiveness of the glass bead applicator in delivering beads to the line with precision, both laterally and longitudinally.

    - Assess the effectiveness of documented calibration procedures for paint and glass bead application rate.

In addition to the above, the following shall apply to all Type A and B machines:

    - Check that dual guns are fitted for simultaneous single line application.

    - Confirm that read-out equipment is fitted as specified.

    - Assess traffic control measures against the appropriate AS/NZS1742 standard requirements. Specifically, determine the effectiveness of lead and pilot vehicles where specified.

    - Assess the ability of the operator to control the paint wet film thickness within the specified range, by observation for a minimum period of 10 minutes.

    - Measure the retroreflectivity of line marking produced, in accordance with TP907.

    - Where data loggers are not fitted, carry out audit of contractors application rate verification process as detailed in Table 3, as appropriate.

Table 3 – Contractor’s Records

| Criteria | Data Source | Action | Frequency |
| --- | --- | --- | --- |
| Paint/ glass bead | Plastic bag records | View/ document | once/ month/ Contractor |
| Application rates | Test panel records | View/ document | once/ month/ Contractor |
|  | Contractor material consumption records | View/ document | once/ month/ Contractor |

    - The application rates shall be as detailed in Table 4. It should be noted that these figures assume no application losses. Spray application will commonly produce losses of the order of 10 - 25%, which must be allowed for when reconciling usage data. Plastic bag target figures should be determined in accordance with TP946.

Table 4 – Theoretical Application Rates

*100mm wide line

| Paint Consumption |
| --- |
| m2 / litre | Litres / 100m2 | Litres / 1 km* |
| 2.6 to 3.3 | 30 to 38 | 30 to 38 |
|  | Bead Usage |  |
| kg / litre | kg / 100m2 | kg / 1 km* |
| >= 0.92 | >= 27.5 | >= 27.5 |

5.2.18	Determine the accuracy of placement and dimensions of markings, and for new work, the placement relative to spotting or marking out. The tolerances for line marking shall be as detailed in Table 5.

Table 5 – Placement/ Dimension Tolerances

| Type | Detail | Requirement |
| --- | --- | --- |
| New Work | Spotting | +50mm -50mm from seal centre |
|  | Lateral deviation | 25mm from spotting |
| New/ Maintenance | Stripe width | + 10 -0mm |
|  | Stripe length, <12m | +150 -0mm |
|  | Stripe length, >12m | +300 -0mm |
|  | Module length, 12m | +150 -0mm |
|  | Module length, >12m | +300 -0mm |
|  | Edge parallel to centre | +25mm -25mm |
|  | Lane width | +50mm -50mm from correct width |
| Maintenance | New over old, lateral | <10mm |
|  | New over old, longitudinal | +150 -0mm |

    - Verify by visual night assessment that work has been adequately protected. Inadequate retroreflectivity within 48 hours of application, is an indicator of trafficking prior to curing, and shall be treated as non-conforming product. Poor retroreflectivity performance shall be checked using a calibrated MX 30 reflectometer in accordance with TP907, and shall be greater than 240 mcd/m2/lx.

    - Assess the contractor’s practices, with regard to OHS&W issues, against their quality plans.

5.2.11	Any results found to be outside of specified requirements shall be treated as a non-conformance, and shall be managed in accordance with the Pavement Marking Quality Plan.

# 6.0	DOCUMENTATION

# Complete forms TP948 1 - 4.

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Audit – Line Marking

# Audit No:……………………………………………………………………….......................

Date of audit:     /     /

Location:…………………………………………………………………………………………

……………………………………………………………………………………………………

# Operator Details

Company Name:............................................................................................……………

Contact Name:............................................................................................……………..

Contact No   Telephone:...............................…….  Fax:..........................................….

Operators ......................................................................................................……………

# Plant Identification

Unit Make and Model: ..............................................    Registration No: ………………..

# Assessment

| ITEM | COMMENT |
| --- | --- |
| Materials | Satisfactory/ unsatisfactory |
| Application Rates | Satisfactory/ unsatisfactory |
| Placement, new markings | Satisfactory/ unsatisfactory |
| Placement, maintenance markings | Satisfactory/ unsatisfactory |
| Dimensions | Satisfactory/ unsatisfactory |
| Retroreflectivity | Satisfactory/ unsatisfactory |

Comments:  ……………………………………………………………………………………

……………………………………………………………………………………………………

# Testing Officer.................................................................………………………………......

Form TP948-1, Revn.1.9

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Audit – Line Marking

# PART 1 – MOBILE WORK-SITE MANAGEMENT

| ITEM | OBSERVATION |
| --- | --- |
| Rotating flashing lights |  |
| Flashing arrowboard |  |
| Vehicle signage, machine and other vehicles |  |
| Traffic control devices, where applicable |  |
| Side road signage, where appropriate |  |
| Protection of work |  |
| Application conditions |  |
| Safety jackets |  |
| Ultra-violet management |  |
| Other |  |

# Comments:................................................................................................……………

Testing Officer :...... .............................…………………………………………………..

Form TP948-2, Revn.1.9

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Audit – Line Marking

# PART 2 - APPLICATION

# Audit No:.............…………………………………………………........

Date of audit:     /     /

| MATERIALS – PAINT |
| --- |
| Product |  |
| Approved product |  |
| Batch No. |  | Sample No. |  |
| Non-volatiles by mass, % |  | Density, kg/l |  |

| MATERIALS - GLASS BEADS |
| --- |
| Product |  | Approved product |  |

| APPLICATION RATES – CONTRACTOR RECORDS |
| --- |
| Date |  | Location |  |
| Paint, m2/ l |  | Glass beads, g/ m2 |  |

| PLACEMENT |  |  |
| --- | --- | --- |
| New Work | Spotting |  | Lateral deviation |  |
| New/ Maintenance | Stripe width |  | Stripe length, <12m |  |
|  | Stripe length, >12m |  | Module length, 12m |  |
|  | Module length, >12m |  | Edge parallel to centre |  |
|  | Lane width |  |  |  |
| Maintenance | New over old, lateral |  | New over old, longitud’l |  |

| RETROREFLECTIVITY |
| --- |
| Location |  | Exposure Period, days |  |
| Visual assessment |  | Result, mcd/ m2 /lx |  |

Testing Officer:...………………………………………….............………..........................……….

Form TP948-3, Revn.1.9

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Audit – Line Marking

# PART 2 - APPLICATION

REPORTING

| Data Required | Comment |
| --- | --- |
| Location or lot number |  |
| Total Volume of paint consumed per day or part thereof |  |
| Accumulated length of each type of line marked per day |  |
| Actual paint wet film thickness, minimum 30 readings per gun |  |

Testing Officer:	………………………………………………………………………………………

Form TP948-4, Revn.1.9