1.0	PURPOSE

This procedure describes the process of test for, and measurement of, the penetration resistance of a road surface to a standard impact. Data from the test is used to estimate the likely embedment of sealing aggregate into the road under service conditions. The test may be conducted on a random basis, or to evaluate specific areas of pavement.

2.0	REFERENCES

Determination of stability and flow - Marshall procedure, AS 2891.5.

Design of Sprayed Seals, AUSTROADS July 1990.

Site Selection by Stratified Random Technique, TP061.

3.0	DEFINITIONS

Road surfaces: includes road bases, prime or primer seals and existing seals.

Soft seals: seals are considered to be soft when the ball penetrates into the seal under the static weight of the hammer.

Standard summer road surface temperature: a temperature derived from the average maximum air temperature for the month of January by means of the conversion graph in Figure 2 of the AUSTROADS Design of Sprayed Seals (1990) procedure.

4.0	APPARATUS AND MATERIALS

4.1	Apparatus

- Standard Marshall compaction hammer as specified in AS 2891 Part 5 Determination of stability and flow - Marshall procedure.

- 19.0mm case hardened steel ball bearing

- Thermometer graduated in oC (0-100 oC) suitable for measuring road or pavement temperature.

- Circular tripod (or equivalent) with moveable cross bar and dial gauge (0.5mm units) or steel rule (0.5mm units). Refer figures 1&2.

4.2	Materials

Nil.

5.0 	SAMPLING AND SAMPLE PREPARATION

Nil.

6.0	PROCEDURE

6.1	Ball Penetration Measurement

6.1.1	Identify the section of road to be tested.

6.1.2 	If the testing is to be conducted at random, select the required number of test locations using DPTI Test Procedure TP349, Site Selection by Stratified Random Technique.

6.1.3	Place the ball on the selected site, or if it will not remain stationary, as close to it as possible.

6.1.4	Place the circular tripod (or equivalent) and cross bar in position over the ball and take an initial reading of the distance between the cross bar and the top of the ball. Record this distance (d1) to the nearest 0.5mm.

6.1.5	Remove the cross bar, while leaving the tripod in place to provide a fixed reference level.

6.1.6	Rest the base of the compaction hammer on the ball and apply one blow by raising the sliding weight to the top and allow it to fall.

6.1.7	Remove the compaction hammer and place the cross bar back in position. Measure distance from the cross bar to the top of the ball and record the distance (d2) to the nearest 0.5mm.

6.1.8	Record the difference between the two readings (d2 - d1) as the ball penetration.

6.1.9	Repeat steps (3) to (8) at the other sites.

6.2	Temperature Correction for Sealed Pavements

6.2.1	If the section of pavement is already sealed or primer sealed, record the temperature of the road surface for each reading.

7.0	CALCULATIONS

7.1	For tests conducted on existing seals or primer seals, correct the average ball penetration taken at the temperature of test, for the temperature most prevalent in the summer months, using the following formula.

Pen Ts = Pen Tt - K (Tt - Ts)

where:

Pen Ts = Penetration at standard summer road surface temperature for the location (mm).

Pen Tt = Penetration depth at the time of test (mm).

Ts = Standard summer road surface temperature of the road for the location (oC). This is determined by selecting the nearest location from Table 1 Standard Summer Road Surface Temperatures.

Tt = Temperature of the road surface at the time of test (oC).

K = Temperature susceptibility of penetration (mm/oC)

K factors recommended are:

- single and multiple seals (not fatty) 		0.04 mm/oC

- primer sealed surfaces (not fatty)		0.06 mm/oC

- fatty roads and asphalt surfacings		0.08 mm/oC

8.0	PRECISION

The uncertainty of measurement has been determined as + x.x of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025.

9.0	REPORTS AND DOCUMENTATION

9.1	Reports

Report the mean ball penetration (Pen Tt), or the mean temperature adjusted ball penetration (Pen Ts) to the nearest 0.1mm.

9.2	Documentation

Form TP349-1 (DPTI use only)

Figure 1

Tripod, Cross Bar and Ball Bearing

Figure 2

Tripod, Cross Bar and Ball Bearing, Assembled

Table 1

Standard Summer Road Surface Temperatures (Ts)

| Location | Ts | Location | Ts | Location | Ts |
| --- | --- | --- | --- | --- | --- |
| Adelaide | 45 | Kuitpo | 40 | Pt Augusta | 55 |
| Andamooka | 60 | Kyancutta | 55 | Pt Lincoln | 40 |
| Belair | 45 | Lameroo | 50 | Pt Pirie | 50 |
| Berri | 50 | Leigh Creek | 60 | Renmark | 55 |
| Cape Northumberland | 35 | Lenswood | 40 | Robe | 35 |
| Ceduna | 45 | Loxton | 55 | Roseworthy | 50 |
| Clare | 50 | Lucindale | 45 | Snowtown | 50 |
| Cleve | 45 | Maitland | 45 | Stirling | 40 |
| Coober Pedy | 60 | Marla | 60 | Strathalbyn | 45 |
| Coonawarra | 45 | Meningie | 40 | Streaky Bay | 50 |
| Edinburgh | 50 | Minnipa | 50 | Tailem Bend | 50 |
| Elliston | 40 | Mt Barker | 45 | Victor Harbor | 40 |
| Eudunda | 45 | Mt Burr | 40 | Waikerie | 55 |
| Fowler’s Bay | 40 | Mt Gambier | 40 | Warooka | 45 |
| Georgetown | 50 | Murray Bridge | 45 | Whyalla | 50 |
| Hawker | 55 | Myponga | 45 | Williamstown | 45 |
| Kadina | 50 | Naracoorte | 45 | Woomera | 55 |
| Kapunda | 50 | Nuriootpa | 45 | Yongala | 50 |
| Keith | 50 | Padthaway | 45 | Yunta | 55 |
| Kimba | 50 | Parndana | 40 |  |  |
| Kingscote | 35 | Penola | 45 |  |  |

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights (08) 8260 0230, GPO Box 1533 Adelaide SA 5001

Technical Services Group

Procedure

DETERMINATION of PAVEMENT HARDNESS

BALL PENENTRATION TEST

FORM TP349-1

PROJECT: ……………………………………………………………………………………..

ROAD: ……………………………………………………………..  ROAD NO: ……………

SECTION: ……………………………………………………………………………………..

SURFACE TYPE: …………………………………………………………………………….

| Chainage | Lane | Offset | P/ Temp Tt (oC) | Initial Dist (mm) | Final Dist (mm) | Penetration Pen Tt (mm) | Penetration Pen Ts (mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Mean |  |  |

Pen Ts = Pen Tt - K (Tt - Ts)

| Pavement Type | K factor |
| --- | --- |
| Single and multiple seals (not fatty) | 0.04 mm/oC |
| Primer sealed surfaces (not fatty) | 0.06 mm/oC |
| Fatty roads and asphalt surfacings | 0.08 mm/oC |

Mean Pen Tt :………………….                                                     Mean Pen Ts : ………………….

Comments: ………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………………

Operator:……………..……….      Checked By: ………………..……….      Date: ……………………..

Form TP349-1, Revn. 1.6