The procedure shall be as described in Procedures TP143 except where modified or clarified as shown below.

•	Lime shall be added to the dry prepared soil mass based on a required percentage of dry mass of soil.

•	The lime/soil mixture shall have water added and be cured for 24 hours at approximately plastic limit consistency.

•	The cured mixture shall then be dried at a temperature not exceeding 60oC.

•	The Atterberg limit tests shall then commence.

Precision

The uncertainty of measurement has been determined as + x.x of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025.