The procedure shall be as described in Procedures AS 1289.5.1.1 or AS 1289.5.2.1 except where modified or clarified as shown below.

•	Sample preparation shall be as described in Procedure TP104.

•	Cement shall be added to the soil/water mixture as required.

•	Moisture content shall be determined as a percentage of dry mass of soil plus cement.

•	Cement content is reported as a percentage of dry mass of soil.

•	The compaction test may be performed after a delay depending on construction procedure simulation but normally not exceeding one hour.

Precision

The uncertainty of measurement has been determined as + x.x of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025.