1.0	SCOPE

This procedure covers the determination of the permeability of both conventional and specialised Portland cement concrete to chloride ions.

2.0	REFERENCES

Rapid Determination of the Chloride Permeability of Concrete ASTM C1202

3.0	DEFINITIONS

As detailed in the references.

4.0	APPARATUS AND MATERIALS

Apparatus

- Test cells.

- Monitor unit for current, voltage and temperature.

- Voltage generator.

Materials

- NaOH solution (3.0% by mass)

- NaCl solution (0.3N)

5.0	SAMPLING AND SAMPLE PREPARATION

As detailed in Procedure to be followed.

6.0	PROCEDURE TO BE FOLLOWED

- The procedure shall be as described in ASTM C1202 except where modified or clarified as shown below.

- Deionised water will be used instead of boiled tap water when conditioning samples in desiccator.

- A neoprene gasket shall be used to seal between the cell and the specimen in place of the silicon sealant, in conjunction with the adjustable frame supplied.

- The electrode grids need not be soldered to the shim.

- The electrode cell need not be bonded to the cell.

- The cell shall be assembled as required in the procedure with the added brace/frame holding all items in place.

- Sample details will be entered into Eword Developed software (CCP Monitor) prior to testing.

- Recording of current, voltage and temperature during test will be performed by digital recorder using CCP Monitor software

- CCP Monitor at the conclusion of test will automatically calculate results and generate a test report and letter.

- Minimum and Maximum ambient air temperature must be recorded onto Laboratory Ambient Temperature Check form at completion of test.

7.0	CALCULATIONS

Plot a graph of current (amperes) vs time (seconds) and integrate the area underneath the curve to obtain the ampere - seconds, or coulombs, of the charge passed during the test. (CCP Monitor)

8.0	PRECISION

The uncertainty of measurement has been determined as + 10.0% of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025.

Uncertainty of Measurement determined by and for DPTI Technical Services Group, Field Services Section.

9.0	REPORTS AND DOCUMENTATION

9.1	Reports

Work and report sheets - Rapid Determination of the Chloride Permeability of Concrete.

Reports attached to this TP are generated by CCP Monitor software and are for example purposes only and are not to be used when generating a report.

9.2	Documentation

Laboratory Ambient Air Temperature Check

Laboratory Ambient Air Temperature Check

Rapid Determination of the Chloride Permeability of Concrete

TP541, ASTM C1202

| Date | Min Temp 20oC | Max Temp 25oC | Thermometer ID | Recorded by | Comments |
| --- | --- | --- | --- | --- | --- |

Rapid Determination of the Chloride Permeability of Concrete

Laboratory Ambient Air Temperature Check

Rapid Determination of the Chloride Permeability of Concrete

(TP541, ASTM 1202)

# Certificate Number:  C-XXXX-XX

Client Details:

| Organisation: Contact: Address: |  |
| --- | --- |

Sample Details:

Project Name: Cured by client: Specimen Type: Steel Reinforcing: Specimen Conditioning at testing laboratory: Concrete Class: Location of Specimen within core or cylinder: Concrete Mix Details:

| Cast Date |  |  | Date of Test | Age at Test (days) | Total Charge Passed (Coulombs) | Maximum Current (mA) | Chloride Perm. Class | Max Temp (ºC) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Field | Lab WH - |  |  |  |  |  |  |

| Charge Passed (Coulombs) | Chloride Permeability | The uncertainty of measurement has been determined as ± 10.0% of the test result, at a confidence limit of 95% with a nominal coverage factor of 2, when calculated in accordance with the accreditation requirements as detailed in AS/ISO 17025. |
| --- | --- | --- |
| >4 000 2 000 – 4 000 1 000 – 2 000 100 – 1 000 < 100 | High Moderate Low Very Low Negligible |  |

Signature:	    Print Name:

Title:  	    Date:

Signatory.

# Rapid Determination of the Chloride Permeability of Concrete

# (TP541, ASTM 1202)

Client Details:

| Organisation: Contact: Address: |  |
| --- | --- |

| Sample Details: | Test Details: |
| --- | --- |
| Project Name: Cured by client: Type of Specimen: Cast Date: Steel Reinforcing: Specimen Conditioning at testing laboratory: Concrete Class: Location of Specimen within core or cylinder: Concrete Mix Details: | Location in Structure: Vacuum: Soaking in Degassed water 18hrs: Preparation Date: Test Date: Age at Test: Test Duration: |

Cell Details:

Cell No: Cell No. Field ID No: Test Specimen Dimension: ht. XX (mm) x diam. XX (mm) Lab ID No:

| Time | Time Elapsed (mins) | Cell Current (mA) | Power Supply (V) | Cell Voltage (mV) | Temp (ºC) |
| --- | --- | --- | --- | --- | --- |

Power Supply ID 127/010 Data Logger ID 028-010

Coulombs Passed Q= 900(I0 + 2I30 + 2I60 +..+ 2I300 + 2I330 + I360)

# Tested by:

Calculated by: Computer	   Checked by:	   Date: ..................

# Text boxes

Specimen ID

RAPID DETERMINATION OF THE CHLORIDE PERMEABILITY OF CONCRETE

Sample Number:

Test Method TP541, ASTM C1202-12

DPTI Sample No.

0

50

100

150

200

250

300

0

5000

10000

15000

20000

Time Elapsed (sec)

Cell Current (mAmps)

Area =

(Area x 0.9)/1000 =

Coloumbs